## Slide 1
The Role of Vibrational Excitations in N2 Dissociative Chemisorption on Ru(0001) for Catalytic Processes
Floris van den Bosch N. Gerrits, J. Meyer. Leiden University

## Slide 2: Heterogeneous Catalysis
Highly activated
Extreme reaction conditions
High energy usage

## Slide 3: Plasma Catalysis
Efficient Activation
Instant on/off switching
Mechanism poorly understood

## Slide 4: Plasma-Surface Interactions
Bogaerts, A. et al. ACS Energy Lett. (2018)

## Slide 5: Vibrational Excitations
Energy channel depends on input power
Vibrational Excitations are major energy channel
Vibrations are long-lived
Bogaerts, A. et al. ACS Energy Lett. (2018)

## Slide 6: Nitrogen Dissociation
N2 dissociation is rate-limiting step
Ru(0001) surface lowers energy barrier to ~2 eV
Rate constant

## Slide 7: State-specific Rate Constants
Introduce vibrational quantum number dependent rate constants
Mehta, P. et al. Nature Catal. (2018)

## Slide 8: Fridman-Macheret Model
Mehta, P. et al. Nature Catal. (2018)
Fridman, A., “Plasma Chemistry”, CUP (2008)
Microkinetic Modelling
Reducing energy barrier by fraction of Vibrational Energy
Fridman
Macheret

## Slide 9: Quasi-classical Trajectories
Molecular Dynamics
  Quantized initial state
Surface motion
  Neural Network Potential1
Computing Reaction probabilities
  Incidence energy
  Vibrational quantum number
1Shakouri, K. et al. JPCL (2017)

## Slide 10: Vibrational Efficacy
Vibrational excitation increases reactivity
Excitation corresponds to Energy shift
Vibrational Efficacy:
Dissociation Probability

## Slide 11: Vibrational Efficacy
Dissociation Probability
Vibrational Efficacy

## Slide 12: Rates from Dynamics
Substitute Vibrational Efficacy into Fridman-Macheret equation
Fridman
Macheret
Dynamics
Vibrational
Efficacy

## Slide 13: Take Home Message
Vibrational Excitations have major influence on reaction rates
Even for Thermal Catalysis Vibrational Excitations dominate
Dynamical effects lower base reactivity
Fridman
Macheret
Dynamics
Vibrational
Efficacy

## Slide 14: Probabilities from Dynamics

## Slide 15: Dissociation Probabilities

## Slide 16: Vibrational Distribution
Treanor, C. E. et al. JCP (2003)

## Slide 17: Vibrational Quantization
Wavefunction → Classical Oscillation

## Slide 18: Potential Energy
Vibrational Momentum
- After the bend
Incident Momentum
- before the bend

## Slide 19: Thermal Contributions

## Slide 20: Plasma Contributions

## Slide 21: Thermal Vibrational Efficacy
Kedalo, Y. M. et al. JPCC (2023)